| APPROVALS | DATE | REV | DCN NO. | BY | CHECK | DCC | DATE |
| --- | --- | --- | --- | --- | --- | --- | --- |
| AUTHOR: Margot Phelps | 01/13/11 | V2 | E1100039-x0 |  |  |  |  |
| CHECKED: |  |  |  |  |  |  |  |
| APPROVED: |  |  |  |  |  |  |  |
| DCC RELEASE |  |  |  |  |  |  |  |

A patterned gold coating is to be deposited onto one face of the Compensation Plate, using a mask provided by LIGO. The Compensation Plate (CP) is a cylindrical fused silica substrate, 340 mm diameter x 100 mm thick with no bumper holes; see LIGO-D1000979-v2 for the detailed drawing of the CP.

Applicable Documents

LIGO-D1000981-v2 Compensation Plate Barrel Coating Drawing

LIGO-D080177-v4 Compensation Plate ESD Pattern-Face

LIGO-D1000979-v2  COC TCP Substrate

Coating Specifications:

Side S1 (refer to D080177-v4 for the pattern drawing) is to be coated with an Electro-Static Drive (ESD) pattern using the Caltech supplied mask.

Underlayer: 500 Angstroms (nominal) of inconel or other suitable material to provide adhesion.

Gold coating: 1000 Angstroms (nominal) gold.

Uniformity: Coating thickness should be uniform to approximately 25%.

Mask registration: The mask should be centered on the CP to within 0.5 mm. Note: The outer diameter of the mask pattern is 336 mm; the diameter of the CP is 340 mm, with a 2 mm chamfer around its perimeter. Therefore, given the tolerances specified, the mask pattern may overlap the chamfer by as much as 0.5 mm.

Durability: The coating must be able to withstand soldering, using an Indium-Silver solder, at a temperature of 220-240 deg C.