| APPROVALS | DATE | REV | DCN NO. | BY | CHECK | DCC | DATE |
| --- | --- | --- | --- | --- | --- | --- | --- |
| AUTHOR: V. Parames | 01/23/08 | A | E080048-A |  |  |  |  |
| CHECKED: G Billingsley | 04/04/08 | A |  |  |  |  |  |
| APPROVED: |  |  |  |  |  |  |  |
| DCC RELEASE |  |  |  |  |  |  |  |

Applicable Documents

LIGO-D080055-A 		AdLIGO ETM Mirror Blank

MIL-G-174-B 			Glass, Optical

Requirements

Physical Dimensions 			per LIGO- D080055-A AdLIGO ETM Mirror Blank

Clear Aperture 				Central 200 mm

Serial Number	Blanks shall be serialized as ETMXX, where XX increments starting at 01

Material					Low Inclusion Fused Silica

Final shaping	Shaping shall be performed using a progression of grit size ending with a 320 or smaller grit tool.

Defect depth 				Maximum on any surface or corner is less than 0.5 mm

Homogeneity	≤ 3.0 x 10-6 P-V in the clear aperture
after subtracting tilt and power

Birefringence				≤ 5 nm/cm

Bubble and Inclusion Cross section 	Total ≤ 0.5 mm2/100cm3

Within the clear aperture 			Inclusions with a diameter of 80 m or less are not included

in the total.

| Specification | Method | Frequency of Inspection | Data Delivered |
| --- | --- | --- | --- |
| Physical Dimensions | Visual Inspection | 100% | Diameter Thickness |
| Serial number | Visual Inspection | 100% | Inspection Report included with Certification |
| Material | Process Control Material Certification | 100% | Inspection Report included with Certification |
| Defect depth | Visual Inspection | 100% | Hand sketch indicating location and dimensions |
| Homogeneity | Process Control Material Certification | 100% | Inspection Report included with Certification |
| Birefringence | MIL-G-174 Section 4.4.5 | 100% | Inspection Report included with Certification |
| Inclusions | Visual Inspection | 100% | Hand sketch indicating location and dimensions |

Table 1: MEASUREMENT MATRIX: FREQUENCY AND METHOD