| Originator | Cognizant Engineer | Ext./Phone# | Project | Account Number |
| --- | --- | --- | --- | --- |
| Stephany Foley | Ken Mason | 617-324-5250 | ELIGO SEI HAM |  |

| Dwg/Part Number | Rev | Part Description / Material | Serial Number | Qty |
| --- | --- | --- | --- | --- |
| D972611 D972611 |  | bellows (~20” dia x 9”) / stainless steel bellows (~20” dia x 9”) / stainless steel | 070-SFX 071-SFX | 1 1 |

| Used In (next higher assembly): | SEI |
| --- | --- |

| Vendor Name | PO/Contract Number |
| --- | --- |

Data Package, Receiving/Inspection Remarks:

| Inspection Required Y/N | Visual Damage Y/N | Comments | Name/ Initials | Date Comp. |
| --- | --- | --- | --- | --- |

Process Flow:

| # | Operation | Start Date | Work Area | Instructions | Name/ Initials | Date Comp. |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Clean |  | LLO | these parts were cleaned by the vendor/ bake only by LIGO | T.Evans | 1-5-08 |
| 2 | Vacuum Bake |  | LLO | per 960022, class A, 200°C for 48 hrs | T.Evans | 1-9-08 |
| 3 | Control Point |  | LLO | Review/Approve RGA scan | B. O’Reilly | 1-9-08 |
| 4 | Wrap & Tag vacuum clean parts |  | LLO |  | T.Evans | 1-9-08 |
| 5 | Ship and Deliver/File paperwork |  |  | Please send to: Keep at LLO File one copy of traveler with the DCC. Note: Ship original traveler with these parts. | B.O’Reilly | 1-16-08 |
| END: Go to Traveler or procedure associated with next higher assembly processing |

Special Instructions (Handling/Packaging Constraints, Remarks, etc.) or Notes:

Parts have been chemically cleaned at the vendor. They will need to be BAKED ONLY by LIGO. These bellows are needed when the ISI goes into the HAM Chamber in January 2008.

Since the bellows went in different bake loads I am splitting the traveler. RGA scans will be attached to PDF document.