| Originator | Cognizant Engineer | Ext./Phone# | Project | Account Number |
| --- | --- | --- | --- | --- |
| Stephany Foley | Ken Mason | 617-324-5250 | Enhanced LIGO SEI HAM |  |

| Dwg/Part Number | Rev | Part Description / Material | Serial Number | Qty |
| --- | --- | --- | --- | --- |
| D071100 |  | Blade Springs / Maraging steel |  | 3 |

| Used In (next higher assembly): | SEI HAM |
| --- | --- |

| Vendor Name | PO/Contract Number |
| --- | --- |

Data Package, Receiving/Inspection Remarks:

| Inspection Required Y/N | Visual Damage Y/N | Comments | Name/ Initials | Date Comp. |
| --- | --- | --- | --- | --- |

Process Flow:

| # | Operation | Start Date | Work Area | Instructions | Name/ Initials | Date Comp. |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Clean | 1/9/08 | LLO | clean per LIGO document E960022-B | T.E. | 1/9/08 |
| 2 | Vacuum Bake | 1/10/08 | LLO | per E960022, 200°C, 48 hrs | T.E. | 1/14/08 |
| 3 | Control Point | 1/14/08 | LLO | Review/Approve RGA scan | BO’R | 1/14/08 |
| 4 | Wrap & Tag vacuum clean parts |  | LLO |  | T.E. | 1/14/08 |
| 5 | Ship and Deliver/File paperwork |  | LLO | Post cleaning please send to: LIGO Hanford c/o SEI Decided to keep @ LLO instead for LLO build File one copy of traveler with the DCC. Note: Ship original traveler with these parts. | BO’R | 1/17/08 |
| END: Go to Traveler or procedure associated with next higher assembly processing |

Special Instructions (Handling/Packaging Constraints, Remarks, etc.) or Notes:

These parts are for the enhanced LIGO build at Hanford. Kept these at LLO for LLO build