| Originator | Cognizant Engineer | Ext./Phone# | Project | Account Number |
| --- | --- | --- | --- | --- |
| Andy Stein | Ken Mason | 617-253-7878 | SEI, HAM Enhanced LIGO |  |

| Dwg/Part Number | Rev | Part Description / Material | Serial Number | Qty |
| --- | --- | --- | --- | --- |
| D070494 D070495 D070502 D070503 | A A A A | ALL PARTS ON THIS TRAVELER ARE Aluminum 6061-T6 Cable Clamp Btm, HAM ISI Cable Clamp Top, HAM ISI Bracket, 25-Pin PEEK Bracket, 3-Pin Power PEEK |  | 25 25 15 5 |

| Used In (next higher assembly): | HAM ISI |
| --- | --- |

| Vendor Name | PO/Contract Number |
| --- | --- |

Data Package, Receiving/Inspection Remarks:

| Inspection Required Y/N | Visual Damage Y/N | Comments | Name/ Initials | Date Comp. |
| --- | --- | --- | --- | --- |
| Y |  |  |  |  |

Process Flow:

| # | Operation | Start Date | Work Area | Instructions | Name/ Initials | Date Comp. |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Clean |  | LLO | Per LIGO E960022: -Ultrasonic clean in Liquinox for 10 minutes. -Rinse in distilled water at least 3 times, changing the rinse water every time. -Ultrasonic clean in methanol for 10 minutes | T.E. | ?? |
| 2 | Vacuum Bake |  |  | Per LIGO 960022, 120°C for 48 hrs | T.E. | ?? |
| ? | Control Point |  |  | Review/Approve RGA scan | BO’R | 2-19-08 |
| 4 | Wrap & Tag vacuum clean parts |  |  |  | H.O. | 2/20/09 |
| 5 | Ship and Deliver/File paperwork |  |  | To be used at LLO site. No shipping required. File one copy of traveler with the DCC. Note: Ship original traveler with these parts. | BO’R | 4/22/08 |
| END: Go to Traveler or procedure associated with next higher assembly processing |

Special Instructions (Handling/Packaging Constraints, Remarks, etc.) or Notes:

These parts are for the Enhanced LIGO build at the Livingston site.