| Originator | Cognizant Engineer | Ext./Phone# | Project | Account Number |
| --- | --- | --- | --- | --- |
| Tom Evans | Ken Mason | (509)372-8116 | Enhanced LIGO SEI HAM |  |

| Dwg/Part Number | Rev | Part Description / Material | Serial Number | Qty |
| --- | --- | --- | --- | --- |
|  |  | 3/8-24 x 2” SHCS Ag plated with vented washers |  | ~30 |

| Used In (next higher assembly): | SEI HAM |
| --- | --- |

| Vendor Name | PO/Contract Number |
| --- | --- |

Data Package, Receiving/Inspection Remarks:

| Inspection Required Y/N | Visual Damage Y/N | Comments | Name/ Initials | Date Comp. |
| --- | --- | --- | --- | --- |

Process Flow:

| # | Operation | Start Date | Work Area | Instructions | Name/ Initials | Date Comp. |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Clean |  | LLO | clean per LIGO document E960022-B | T.E. | 2-?-08 |
| 2 | Vacuum Bake |  | LLO | per E960022, 200C, 48 hrs | T.E. | 3-3-08 |
| 3 | Control Point |  | LLO | Review/Approve RGA scan | BO’R | 3-4-08 |
| 4 | Wrap & Tag vacuum clean parts |  | LLO |  | T.E. | 3-4-08 |
| 5 | Ship and Deliver/File paperwork |  |  | Please send to: LIGO Livingston File one copy of traveler with the DCC. Note: Ship original traveler with these parts. | BO’R | 4-21-08 |
| END: Go to Traveler or procedure associated with next higher assembly processing |

Special Instructions (Handling/Packaging Constraints, Remarks, etc.) or Notes:

After cleaning these parts, give to Joe Hanson for LLO HAM6 ISI build.