| APPROVALS | DATE | REV | DCN NO. | BY | CHECK | DCC | DATE |
| --- | --- | --- | --- | --- | --- | --- | --- |
| AUTHOR: L. BARSOTTI | 12-16-10 |  |  |  |  |  |  |
| CHECKED: |  |  |  |  |  |  |  |
| APPROVED: P. FRITSCHEL |  |  |  |  |  |  |  |
| DCC RELEASE |  |  |  |  |  |  |  |

# Description

1” Ø  and 2” Ø  95% beam splitters @ 1064nm

# Material

Corning HPFS 7980 (high purity fused silica, UV grade)

Grade 0A (Low inclusion class: <0.3 mm² cross section, 0.1 mm max. size;

Homogeneity < 1ppm)

# Dimensions, Surface Roughness and Figure

E1000871-v1-01

1"Ø +.000/-.005" X .250" ± .020" tk., Plano / Plano

Wedge: 30 arc minutes ± 5 arc minutes                                                                                                  Surface Roughness:

Side 1

Super polish

Surface Roughness: <1Å RMS in CA

Surface Quality: 10-5

Side 2

Commercial Polish

Surface Roughness: <5Å RMS in CA

Surface Quality: 20-10

Surface Figure:

Side 1

Flat < λ/10 at 632.8 over central 80%

Side 2

Flat < λ/4 at 632.8 over central 80%

E1000871-v1-02

2"Ø +.000/-.005" X .375" ± .020" tk., Plano / Plano

Wedge: 30 arc minutes ± 5 arc minutes                                                                                                  Surface Roughness:

Side 1

Super polish

Surface Roughness: <1Å RMS in CA

Surface Quality: 10-5

Side 2

Super Polish

Surface Roughness: <1Å RMS in CA

Surface Quality: 20-10

Surface Figure:

Side 1

Flat < λ/10 at 632.8 over central 80%

Side 2

Flat < λ/5 at 632.8 over central 80%

# Coating

Wavelength: 1064nm

Angle of incidence: 45°

Side 1

R=95% ( 0.5% for p polarization

Side 2

AR coating, R < 0.1% (best effort) for p-polarization

Arrow pointing to side 1, serial numbers and registration marks shall be scribed or etched on the barrel of the optic for in-vacuum use.

# Coating vendor to provide:

  - 1. Two spectrophotometer graphs of the reflectance and transmittance of the HR coatings; one covering the spectrum from 530nm to 1200nm; the other, with increased sensitivity, showing wavelengths from 900nm to 1100nm

            - 2. Spectrophotometer graphs of the reflectance of the AR coating taken as cited above.