| AUTHOR(S) | DATE | Document Change Notice, Release or Approval |
| --- | --- | --- |
| Jeff Lewis (D. Coyne update and Calum Torrie update) | 14 Feb 2024 | see LIGO DCC record Status |

# Scope

This document defines the requirements for music wire to be supplied for use in LIGO suspension systems.

# Requirements

## General

- Material: Music Wire per ASTM A 228/A 228M chemical only

- Material: Bare music wire no coating.

- Temper: Stress Relieved

- Minimum Tensile Strengths: Refer to table on 1 on page 2 of ASTM A 228/A 228M.

- Further on Minimum Tensile Strengths: for typical LIGO wire diameters in the range    0.0078 inches [0.2mm] up to 0.0394 inches [1 mm] the following can be used as a guide:

| Diameter | Minimum Tensile Strength |
| --- | --- |
| inches | mm | ksi | Gpa |
| Typical LIGO wire diameters in the range 0.0078 [0.2mm] up to 0.0394 inches [1 mm] can use the following2. | 290 | 2.00 |

- Diameter tolerance (inches):

  - 0.0030 to 0.0109  +/-0.0001

  - 0.011 to 0.019  +/- 0.0003

  - 0.020 to 0.050  +/- 0.0005

- Minimum 8 inch cast at 12-inch length.

## Processing

- Clean gloves must be worn at all times.  (No bare hands touching the wire)

- Wire must be fresh drawn within 2 weeks of shipment

- Wire must be free of oil and grease and must not be used during the manufacturing process

## Inspection and Documentation

- Wire shall be free of rust, scale, corrosion, spotting artifacts, die marks, pits, and scratches visible at 10X magnification

- Provide Material Certifications

- Provide Certificate of Conformance to Purchase Order requirements

## Packaging

- Wire shall be shipped on 12 inch diameter spools

- Wire shall be sealed in a container with a molecular sieve desiccant consistent with LIGO specification E1300075

- Desiccant shall be added inside plastic shipping bag

- Purge plastic shipping bag with inert gas before sealing

- Double bag

## Selecting wires for suspensions [Internal to LIGO]

- Generally music wire used in a suspension is selected for use at 1/3 (one-third) of the Minimum Tensile Strength* or Breaking Stress of the wire. Refer to the DCC for further details and examples of use.

*Note that the Minimum Tensile Strength value should be used even if the music wire has an Ultimate Tensile Strength higher than the Minimum Tensile Strength.

- Take care when designing the associated clamping mechanism; refer to existing LIGO clamp (clamp-wire-clamp) designs) on the DCC.

# Footnotes

Industry coats Music Wire with phosphate for corrosion resistance and lubricity. Phosphate is bad for LIGO’s ultra-high vacuum, hence why it is important to call out bare music wire no coating.

2  LIGO specification based on typical numbers in ASTM A 228/A 228M across range specified.

Internal LIGO documents refer to LIGO-E1100187-v5 and LIGO-T1100120-v2.