## Slide 1: AlGaP coatings plans: growth
Si
AlGaP
GaP
Si
AlGaP
Si
GaP
Si
Nucleation
Structure | Purpose | Characterization
AlGaP/GaP mirrors on Si | Study interface effects: vary # of mirror pairs | Mechanical loss (disk, cantilever) RT and low T absorption XRD, TEM, AFM
AlGaP on Si | Study bulk AlGaP properties | Mechanical loss (cantilever) XRD, TEM, AFM, nanoindentation
GaP on Si | Study bulk GaP properties Control defect annihilation | Mechanical loss (cantilever) RT and low T absorption XRD, TEM, AFM, nanoindentation
Nucleation layer (10 ML) on Si | Reduce atomic-scale defect formation | AFM, TEM (EELS, HAADF), RDS
AlGaAs/GaAs on GaAsP on Si | Study effect of dislocations on mech loss and absorption | Mechanical loss Absorption XRD, TEM
Si
GaAsP
AlGaAs
GaAs

## Slide 2: Crystalline coating loss measurements at Glasgow
Glasgow measurements of initial MBE GaP/AlGaP coating on going
  Collaboration with Stanford ongoing – hopefully a second MBE GaP/AlGaP coating for further studies of this material
  GaP single layer coatings on silicon cantilevers to be made by Kelvin Nanotechology (KNT) and measured at Glasgow
  Study multilayer physics from single layer measurements
Silicon disk to be sent to Garrett Cole to have AlGaAs coating transferred on to it
  Disk will be measured at Glasgow throughout the temperature range 12-300K